## Slide 1: SCALING of an assisted PHYTOSTABILIZATION FROM GREENHOUSE TO FIELD-SCALE AT THE IRON KING MINE-HUMBOLDT SMELTER SUPERFUND SITE Juliana Gil-Loaiza, M.S. student Dept. of Soil, Water and Environmental Science University of Arizona,Tucson AZ, USA.
U.S. EPA Hardrock Mining Conference 2012:
Advancing Solutions for a New Legacy
April 4th, 2012
Denver, CO
April, 2010
September, 2011

## Slide 2: Mine Tailings
High concentration of metals
From acidic to neutral pH
Poor soil structure
Lack of nutrients
Low microbial community
Barren surface
Risk Exposure
Human and
Environment
Water Erosion
Wind Erosion
Iron King Mine Tailings
2

## Slide 3
Site description
Iron King Mine-Humboldt Smelter Site (IKMHSS)
Superfund Site by Environmental Protection Agency (EPA) in 2008.
PHYTOSTABILIZATION
Vegetative cap to stabilize metals in the root zone.
Reducing wind and water erosion.
WWW.azdeq.gov
Source:http://www.azdeq.gov/environ/waste/sps/
Tucson
Tucson
Town of Dewey-Humboldt
ARIZONA
Phoenix
3
  PROBLEM
  Arsenic and lead up to 4000 mg/kg

## Slide 4
Topsoil cap
Gravel layer or
Bentonite-cement seal
Disadvantage
High cost for large tailing areas
Low durability in arid and semi-arid areas
phytostabilization
Tailings
4
Liability
Cost-effective
Planting directly into the tailings
Capping

## Slide 5
phytostabilization
Iron King Mine tailings
Low pH
High Salinity
Low Nutrients
Plants don’t grow
High metals
Mendez and Maier, 2008. Environ. Health Perspec.
5

## Slide 6
Greenhouse
Compost
Lime
Irrigation
Buffalo grass (BG) –Buchloe dactyloides
Arizona fescue (AF) –Festuca arizonica
Quailbush (QB) – Atriplex lentiformis
Mountain mahogany (MM) –Cercocarpus montanus
Mesquite (MQ) –Prosopis juliflora
Catclaw acacia (AC) – Acacia greggi
Solis-Dominguez F. A., et.al.. 2012, Environ. Sci. Technol.
Amendments
Native plants selection
15 species
6

## Slide 7
Greenhouse
Solis-Dominguez F. A., et.al.. 2012, Environ. Sci. Technol.
Plant Biomass
Neutrophilic heterotrophic and Plant biomass
Not shoot metal uptake, except for Zn in quailbush
7
10% 15% 20%
Buffalo grass

## Slide 8: OBJECTIVE
To determine whether successful results from greenhouse studies can be translated to the field, and also, to identify the parameters that indicate successful phytostabilization at IKMHSS.
8

## Slide 9
METHODOLOGY -Field plot and treatments-
Seeds
Buffalo grass (BG)
Arizona fescue (AF)
Quailbush (QB)
Mountain mahogany (MM)
Mesquite (MQ)
Catclaw acacia (AC)
127 ft
300 ft
N
PHASE I
9

## Slide 10
METHODOLOGY -Field implementation-
2. Site Preparation
3. Sampling
4. Seeding
5. Irrigation
Setup Complete
1. Study Area
10

## Slide 11
CANOPY COVER
Daubenmire frame method
NEUTROPHILIC HETEROTROPHIC BACTERIA
Plate counts on R2A agar
SHOOT METAL UPTAKE
Microwave digestion and ICP-MS analysis
PARAMETERS -Measured-
11

## Slide 12: RESULTS
After 5 and 17 months
of phytostabilization for PHASE I
3
Shoot metal
uptake
2
Neutrophilic Heterotrophic Counts
1
Canopy
Cover
12

## Slide 13: RESULTS -phase I -
1
Canopy
Cover
13
There is no cover vegetation for the unamended control compared with those treated with compost.
Canopy cover is higher than 30% after 5 months for those treated with compost and seeds. Then, after 17 months they have decrease to 20%.
Canopy cover after 17 months looks healthy. And it is more similar to the surroundings.
On those unseeded treatments canopy cover ranges from 7 to 16% due to volunteer plants (plants that grew without having been planted) have established after 17 months.
Canopy Cover

## Slide 14
Unamended irrigated control
20% compost + No Seeds
Sept. 2011
2010
2011
20% compost + Seeds
5 Months
17 Months
1
Canopy
Cover
5 Months
17 Months
14
Off-site
Sept. 2011

## Slide 15
Blooming and seeding after 17 months
Buffalo grass
Quailbush
15

## Slide 16
RESULTS -PHASE i-
2
NHBC
Neutrophilic Heterotrophic Bacterial Counts
16
Unamended control results showed bacterial counts of 102 to second and how they increase 2 or 3 orders of magnitude at time 0 with the rate of compost.
NHBC increase 1 or 2 orders of magnitude with time on those plots treated with compost, after 14 months.
Taking into account that for 0 months we only have tailings, compost and seeds, and after 14 months we have a vegetation cover established, we can see that there is likely an interaction between microorganisms and plants.

## Slide 17
RESULTS -Phase I-
a DATL= domestic animal toxicity limit.
3
Shoot metal
uptake
17
The National Research Council has defined the domestic animal toxicity limits for cattle being 30, 100, and 500 mg/kg for As, Pb, and Zn, respectively.
Metal accumulation in shoot tissue for buffalo grass and quail bush do not exceed the domestic animal toxicity limits at any rate of compost with an exception for zinc in buffalo grass, which is slightly higher.

## Slide 18
April, 2010
September, 2011
September, 2011
18

## Slide 19: SUMMARY

## Slide 20
Phytostabilization was successfully scaled from the greenhouse to the field.
Direct planting achieved a canopy cover equivalent to the surrounding area. We will follow tailings characteristics over time to see if they improve as a medium for plant growth.
Percent canopy cover, neutrophilic heterotrophic bacteria, and shoot uptake of metal(oids) are promising criteria to use in evaluating phytostabilization success.
Phase I –March, 2011-
Phase I –October, 2011-
REFERENCES
Mendez M.O., Maier R.M., 2008. Rev Environ Sci Biotechnol 7:47–59
Epelde L., et al., 2010, Environ Pollut 158:1576–1583
Solis-Dominguez, F. A., et.al.. 2012, Environ. Sci. Technol.,46 (2), pp 1019–1027.
20

## Slide 21
Effect of lime and use of transplants
Stopping irrigation
Self-sustainability of vegetative cap
Metal mobility and bioavailability (Soil-Water-plant)
Relationship between vegetative cover and dust emissions
10-meter dust flux tower (1 of 3) designed to measure meteorological parameters and vertical dust fluxes from the contaminated tailings.
What is next ?
21

## Slide 22
Raina Maier, PI
Jon Chorover, PI
Eric Betterton, PI
Scott White, Field expert
Mary Kay Amistadi
Janae Csavina
Travis Borillo-Hutter
Jason Field
Xiaodong Gao
Funding
NIEHS SRP Grant P42 ES04940
EPA
Leah Butler
Monika O’Sullivan
ADEQ
Brian Stonebrink
North American Industries
Stephan Schuchardt (site owner)
Photos:
Corin Hammond
Juliana Gil-Loaiza
Karis Nelson
Robert Root
Alexis Valentin-Vargas
ACKNOWLEDGMENTS
Corin Hammond
Sarah Hayes
David Hogan
Karis Nelson
Robert Root
Richard Rushforth
Fernando Solis-Dominguez
Lane D. Undhjem
Alexis Valentin-Vargas
University of Arizona
22

## Slide 23: THANKS
Questions
?
**You can follow the field study at :
http://cals.arizona.edu/crops/irrigation/azdrip/BostonMill/IK/photolog.htm
Superfund Research Program University of Arizona
http://superfund.pharmacy.arizona.edu/
Juligil@email.arizona.edu

## Slide 24
Chart: pH by Treatment - Time 0

## Slide 27: METHODOLOGY -Canopy Cover-
Two diagonal transects
Placement of frames and calculation
Daubenmire frame method